Creation Clic System

CREATION CLIC SYSTEM is a synthetic, decorative, flexible, antistatic, abrasion group T floor covering available in planks 17.2x100cm with bevelled edges.

It consists of a transparent wear layer 0.7mm thick, a design film, a compact reinforced under layer. They are compressed and grained at high pressure.

It benefits from a polyurethane surface treatment (PUR), making maintenance easier and eliminating the need for initial polishes.

The overall thickness is 6mm.