MIPOLAM ACCORD

MIPOLAM ACCORD is a monolayer homogeneous flooring with high PVC content calendered and pressed in 2m sheets, with a thickness of 2mm and a weight of ≤ 2850g.

The semi-directional design with colour throughout the thickness is available in 29 references presenting a nice matt finish.

This flooring is recommended for collective buildings making skirtings easier, as well as angles and welding.

The flooring is equipped with EvercareTM the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. This EvercareTM avoids staining of chemical products used in Healthcare like betadine, eosin or anti-bacterial hand gel and increases the durability of the flooring.

This treatment has excellent maintenance characteristics and does not require the application of acrylic polishes.

The flooring is composed of minimum 25% recycled content 100% controlled and is REACH compliant.

This flooring is anti-static (<2kV), fungistatic and bacteriostatic and resistant to the main chemical product used in healthcare (no impact of betadine after 24h).

The product is non reactive to residual indentation with a value ≤ 0,03 mm (EN 433)

The flooring complies with the EN 649 (34-43) offering a group T  wear rating suitable for heavy duty traffic areas and Bfl-s1 fire resistance.

The product emission rate of volatile organic compounds is <10 µg/m3 (TVOC after 28 days ISO 16000-6).