Mipolam Elegance EL5

MIPOLAM ELEGANCE EL5 is a PVC conductive flooring according to European Standard 1081 (104 ≤ Rt ≤ 106) and is available in 2m wide rolls.

It is a 2mm homogeneous product incorporating encapsulated granules throughout the thickness of the product and a conductive backing to ensure optimal and constant conductive properties throughout the product’s full life expectancy.

The product has excellent resistance to static and rolling loads (the floor is classified 34-43 according to European Standard).