TARALAY ELEMENT COMFORT is a multilayered vinyl floorcovering available in 2m wide sheet, with a group T wear rating.

The product comprises a 0.75mm thick, pure vinyl and coloured wear layer throughout the thickness, without a transparent wear layer.

It comprises a Very High Density (VHD) foam and is reinforced with 2 fibre glass grids which yields a 17dB sound insulation rating and a resistance to indentation of 0.07mm.

This flooring is protected by the surface treatment, Protecsol®, with a minimum thickness of 25µm, ensuring easy maintenance and no required polish for the entire lifetime of the product.

It is composed of 47% mineral and inexhaustible materials.

It does not contain any heavy metals or CMR 1&2 components and it is 100% compliant with REACH.

The product emission rate of volatile organic compounds is <70µg/m³ (TVOC after 28 days ISO 16000-6). It is 100% recyclable.