Taralay Initial Comfort

TARALAY INITIAL COMFORT is a foam backed vinyl floorcovering available in 2m wide sheet form and providing high sound insulation (19 dB).

The transparent wearlayer is treated with Protecsol®, a UV cured, antiglazing treatment, which facilitates ease of maintenance and eliminates the use of acrylic emulsion (metallisation).

The product has antistatic properties (AS Class 1).