TARALAY PREMIUM

TARALAY PREMIUM is a multilayered calendered and pressed vinyl floorcovering, with no filler and a group T wear rating, available in 2m wide sheet.

The product comprises a >1mm thick, pure vinyl wear layer incorporating very densely pressed coloured chips, with a mat finishing and without a transparent wear layer.

The product comprises a compact backing which is calandered, pressed and a Very High Density (VHD) foam backing. It is reinforced with a double glass fibre grid yielding a 16dB sound insulation, an indentation resistance of 0.06mm and a rolling heavy loads easiness.

TARALAY PREMIUM is treated with Protecsol®2, a surface treatment obtained by UV laser crosslinking. This Protecsol®2 ensures easy maintenance and eliminates permanently the need for acrylic emulsion (metallisation). It avoids staining of chemical products used in healthcare like iodine alcohol, Betadine, eosin and anti-bacterial hand gel.

It is composed of 40% of minerals and inexhaustible materials.

It is made of 100% controlled recycled materials.

It does not contain any heavy metals or CMR 1&2 and they are 100% compliant with REACH.

On demand, Taralay Premium is available with phthalate free.

The products emission rate of volatile organic compounds is <10µg/m3 (TVOC after 28 days – ISO 16000-6).

It is 100% recyclable.