TARALAY UNI COMFORT

TARALAY UNI COMFORT is an acoustic multi-layered vinyl floorcovering, available in 2m wide sheet, with a group T wear rating.

The product comprises a Very High Density (VHD) foam backing reinforced with a glass fibre and a calendered wearlayer with colour within the 0,65mm thickness.

It offers 17 dB sound insulation and an indentation resistance of 0.11mm. It has a plain coloured design, making it ideal for cut design work.

It is protected by a UV cured surface treatment Protecsol® which facilitates ease of maintenance and eliminates permanently the need of an acrylic emulsion (metallisation).

It does not contain any heavy metals or CMR 1&2 and it is 100% compliant with REACH. The product emission rate of volatile organic compounds is < 70 µg/m3 (TVOC after 28 days – ISO 16000 -6). It is 100% recyclable.